## Introduction to NLO properties of Organic Materials

Light wave =0 cos(t+)

NLO property enables modification of 0, ,  of an optical signal

Why organic materials?

-exhibit large optical nonlinearity

-amenable to optimization of their properties by rational modification their structures at the molecular or supramolecular levels.

1. Basic Concepts

1.1. Microscopic Description of the polarization

h()       =q       displacement of the electron density

()

For small field

() =()Ej()

= linear polarization tensor

For  far from resonance, response is instantaneous.

At optical frequency ~ mainly electronic contribution

At low frequencies, vibrational and orientational mechanisms contribute to

For high 0,  is nonlinear function of . For example, second order materials show

Common approximation (Taylor series expansion)

or

where =the linear polarizability

=the permanent dipole

=the first hyper polarizability (second order polarizability)

=the 2nd hyper polarizability (third order polarizability)

NLO effects becomes more important with increasing

Under normal conditions,

2.2. Macroscopic Description of the Polarization

Analogous to the microscopic polarization, bulk polarization P is given by

=++++·····

: the permanent polarization

: the linear susceptibility of an ensemble of molecules

,: the 2nd & 3rd-order susceptibility, respectively

Relationship between  & ·····

Assume no intermolecular interaction (coupling)

NF(or)

where N is the number of chromophores per unit volume, F the local field factor, and  the orientational factor

# Linear term

Where D is the total electric field within the material and 4is the internal electric field (displacement) created by the induced polarization of charges.

### Two bulk parameters

The effect of light on the polarization of the medium

(n  c/v)

Change of the propagation characteristics of light

#### Second Order Term

SHG ; 1=2, 3=21

SFG ; 3 = 1 +2

DFG ; 3= 1 - 2

Optical parametric generation(OPG) 3= 1 +2

Pockels effect 1=0 (dc)

Note:  second order nonlinearity requires the lack of a center of symmetry

#### Second Harmonic Generation

SHG was reported in 1961 in quartz

Subsitute E = E0cost in the polarization equation.

For efficient SHG

- the quality of material

- the largest  (large ) molecule

- the fundamental and the second harmonic light waves must propagate throughout the material in a synchronous manner,

i.e., n() = n(2) : the phase matching condition

#### Parametric Processes

optical parametric generation

3     1 +2

Which are intense?

By phase matching conditions

(orientation of the material, temp, external field ⇒ n

#### Pockels effects

E2 → n → v changes

~ phase modulator

~ polarization state

~ intensity modulation

We use

rij  (i = 1,2,3, j = 1-6)

#### Third order term

- four wave mixing processes

- no symmetry restriction

THG : three incident waves have the same frequency 

#### Kerr effect

-  or  is + : self focusing

-  or  is - : self dedocusing

- all optical signal processing

#### Degenerate Four-wave mixing

The associated process ;  + - → 

Two beams of light interacting in a 3rd order NLO material will create a refractive index grating. When a third beam is incident on this grating, a fourth beam (the phase conjugated) is diffracted from the grating. It is called four wave mixing.

⇒ phase conjugate optics

Special feature of the diffracted beam

Its path exactly retraces the path of one of the writing beams. As a result, a pair of diverging beams impinging on a phase-conjugate mirror will converge after reflection.

→ using a phase conjugate mirror, distorted optical wavefronts can be reconstructed using a phase conjugated mirror

Electric Field Induced SHG (EFISH)

 + +0 → 2

the most common technique to evaluate  and

= the intrinsic hyperpolarizablity

=

c.f. absorption in SHG, THG, even in DFWM

# Text boxes

h

=0 cos(t+)

: matter consists of e- and  nucleus.

Nucleus is much heavier than e-

Input

=

Static polarization

(optical rectification)

Frequency doubled

SFG

DFG

Kerr effect

THG(3)

Fig6.1 (a) Plots of the electric field of an applied light wave and the induced polarization wave as a function of time, for a linear material; (b) diagram depicting the charge distribution and the polarization in the material as a function of time; (c)plot of the induced polarization as a function of the applied field. (From Ref. 11.)

Fig6.2 (a) Plots of the electric field of an applied light wave and the induced polarization wave as a function of time for a second-order nonlinear material; (b) diagram depicting the charge distribution and the polarization in the material as a function of time; (c) plots of the induced polarization as a function of the applied field, for both linear and nonlinear material.

Fig 6.3 Fourier analysis of a second-order polarization wave (see the text);the induced polarization is similar to the one depicted in Fig.6.2a.

Fig 6.3 Fourier analysis of a second-order polarization wave(see the text);the induced polarization is similar to the one depicted in Fig.6.2a.

Fig 6.5 (a) A planar wave (b) passes through a distorting material that introduces an aberration and (c) the material interacts with a phase-conjugate mirror, creating the phase-conjugate image. (d) When the phase-conjugate wave passes through the distorting material on the reverse path, the original aberration is canceled, producing an undistorted image.(From Ref. 11.)